Lock to prevent coming off of spigot-and-socket joints of Pragma DN/OD pipes-Pragma Lock

- Application:  preventing the coming off of spigot-and-socket joints of Pragma; ensuring water tightness when pipe’s axis displaces horizontally or vertically;

- Raw material used to manufacture the product: virgin material, primary certified by independent institution;

- Material: polypropylene (PP) and synthetic rubber(EDMP);

- Product description:  spigot-and-socket joint locking system, performed by Pragma pipe socket end, EDMP O-ring, EDPM O-ring placed facing opposite the direction of inserting the spigot end into the socket end, Pragma pipe spigot end, Click-ring fitting together with EDPM O-ring.

- Color: sealing ring -black, Pragma pipes -orange; Click ring-orange;

- Nominal diameter: DN/OD 160, 200, 250, 315 and 400;

- Water tightness of the joint: from 0.5 bar   to -0.3 bar. Up to 10ᵒ in pipe’s axis variation;

- Compatibility with PP-B profiled pipes by outer diameter: Yes

- Standards: БДС EN13476-3+А1:2009; БДС EN 1411; БДС EN 12061; БДС ISO 9969; БДС EN 1277;