Modular boxes for infiltration and storage of stormwaters Stormbox II

- Application: for non-pressure detention or retention of storm water. Rainwater can be used for drainage into the soil, controlled discharge to the sewage system or to channels and rivers, reuse, irrigation, etc.

- The system is usable for:

- Infiltration — water is collected in the units during rainfall and allowed to drain away by soaking into the surrounding ground over a substantial period of time after the rain has stopped

- Attenuation — water is collected in the units during rainfall and released at a reduced flow rate through a flow control device, into an appropriate outfall. This reduces peak flows in the watercourse and, therefore, minimizes the risk of flooding

- Combined systems — water is collected in the units during rainfall and able to flow out of the tank via infiltration and through an outlet flow control device into an appropriate outfall

- Product description: basic modular boxes that can be connected(vertically or horizontally), side walls for connecting and flushing, bottom plate, hinge hook connection( without clips).

- Production: The units are manufactured using conventional injection moulding techniques.

- Material:   must be a virgin material PP-B with MFI <6

- Color: Green-Traffic RAL 6024

- Storage factor: min 95,5%

- Net water capacity: 412,6 l

- Dimensions of boxes: width 600mm, length-1200mm, height-300mm.

- Total surface area of opening:  ≥ 50% of the open box area.

- Structure of boxes: cuboid with Five faces (without bottom), with special vertical and lateral reinforcements.

- Type of connection between boxes: Patented connection method without clips-“herringbone” type. Bottom plate is used only on the bottom layer without using clips-installation through pressing.

- Brick bond formation: Yes

- Cutting: The box and the bottom plate are designed in such a way that they may be cut in two halves widthwise.

- Inlets, vertical and horizontal for filling and revision: DN/OD 110, 125, 160, 200 for smooth or corrugated pipes of PE, PP or PVC!

- Adapters for entry to the system on top face: OD 630, ID 425, OD 400, OD 200, for smooth or corrugated pipes of PE, PP or PVC!

- Short term vertical loading on top face:  ≥ 600 kN/m2 (EN 17150:2019)

- Short term lateral loading on side face:    ≥ 100 kN/m2 (EN 17150:2019)

- Long term vertical loading on top face (for 50years):   234.6 kN/m2 (EN 17151:2019)

- Long term lateral loading on side face load (for 50years):  28.8 kN/m2 EN 17151:2019)

- Durability: The boxes, when used in accordance with requirements, will have a life of 50 years when maximal loaded.

- Marking, according the requirements: manufacturer’s logo, product name, material symbol, manufacturing date, box capacity.

- System kit: Infiltration boxes, bottom plates, side walls-for connection or flushing, adapters and geotextile or membrane.

- Installation parameters for areas subject to traffic loads: min. depth-0.8m, max depth-4.15m

- Installation parameters for green areas: min. depth-0.4m, max depth-4.15m

- Compatibility with drainage and sewerage system elements ( manholes and inspection chambers, waste water treatment plants, different types of pipes-smooth or profiled, etc. ): Yes

- Inspection and cleaning: Inspection via CCTV and hydro-dynamically cleaning with a pressure of up to 180 bars.

- Resistance to chemicals: The components of the system are suitable for use in contact with the chemicals likely to be found in rainwater

- Software: Software that guarantees conformity with the standards of product, way of application and methods of calculations for hydraulic and static dimensioning of the boxes (systems for infiltration or storage).

- Standarts: БДС EN 17151; БДС EN 17150; БДС EN 17152-1; AT-15-7731 / 2008 ITB, AT/2008-03-2402 INDiM, BRL 52250

- Certificates and approvals:  KOMO KIWA N.V.K54088/01, IBAK KOKS RIDDERKERK, IBAK retell IPEK, 403388-4 OFI Technologie & Inovation GmbH

- Reuse and recyclability: The product comprises polypropylene that can be recycled.

- Manufactured: conformity  with ISO 9001