POLYPROPYLENE PIPE SYSTEM FOR INFRASTRUCTURAL SEWERAGE PP MASTER TYPE OR EQUIVALENT

- Application: according the applying “Sewage systems design standards”: thermoplastic sewage system for gravity water drainage of house, production or rain sewage;

- Raw material  used to manufacture the product:  virgin material, primary certified by independent institution;

- Production technology:  multilayer extrusion method;

- Type of connection: socket, sealing ring and a support ring that prevents warping and extrication of the sealing ring during insertion of the pipe into the socket;

- Socket, guarantee water tightness and strength of the connection, made from the same material as the pipe, an integral part of each pipe;

- Sealing ring: matrix made of synthetic rubber - an integral part of each pipe.

- Pipe material: polypropylene PP-ML (multilayer polypropylene);

- Outer layer - brown. Polypropylene filled with minerals. High level of elasticity and stiffness, resistance against penetration of foreign objects in the pipe wall. High UV-protection, possibility of outdoor storage. Middle layer - black. Polypropylene. High impact resistance even at very low temperatures. Inner layer - white reflective color. Polypropylene with high chemical, thermal and abrasive resistance. The smooth surface ensures excellent fluid stream;

- Effective pipe length without socket: 1, 3 and 6 m;

- Product Description: three-layer smooth solid wall polypropylene pipe (no foam), light inside layer (enhances the TV inspection), highly abrasion resistant;

- Roughness of the internal layer ≤ 0.015 mm;

- Nominal ring stiffness (SN) ≥ 10kN/m2: proven by a test protocol;

- Ring flexibility ≥30% - proven by a test protocol;

- Water tightness of the connections: proven by a test protocol;

- Nominal Diameter DN: DN/OD 110, DN/OD 125, DN/OD 160, DN/OD 200, DN/OD 250, DN/OD 315, DN/OD 400 and DN/OD 500;

- Readable and resistible marking outside and inside the pipe (necessary for identification of the pipes by TV inspection);

- System: complete certified system – pipes and fittings;

- Compatibility with sewerage system elements ( manholes and inspection chambers, waste water treatment installations, drainage boxes);

- Compatibility with smooth-wall pipes - DN/OD with guarantee water tightness of  the connection;

- Standard: ÖNORM ONR 20513;

- Quality mark: by GRIS;

- Manufacturing: according ISO 9001.

Technical specification: