COMPACT SMOOTH POLYPROPYLENE PIPE SYSTEM FOR INFRASTRUCTURE SEWAGE PP MONO OR EQUIVALENT ACCORDING EN1852-1

- Application: according the applying “Sewage systems design standards”: thermoplastic sewage system for gravity water drainage of house, production or rain sewage;

- Description: single layer, compact, smooth inside and outside polypropylene pipe;

- Raw material used to manufacture the product:  virgin material, primary certified by independent institution;

- Production technology:  extrusion method;

- Type of connection: double socket with two sealing rings or butt welding: proven by a test protocol;

- Socket: double socket, made from the same material as the pipe, guarantee water tightness and strength of the connection;

- Butt welding resisting 10bar pressure - proven by a test protocol;

- Safety Lock - additional rings on both sides of the double socket preventing the escape of the sealing ring during the insertion of the pipe into the double socket;

- Pipe material: polypropylene PP (polypropylene);

- Color: other than black, uniform in terms of hues and saturation;

- Effective pipe length: 6 m;

- Roughness of the internal layer: ≤ 0.015 mm.

- Nominal ring stiffness (SN): ≥ 8kN/m2 or ≥ 10kN/m2 or ≥ 12kN/m2 or ≥ 16kN/m2: proven by a test protocol;

- Water tightness of the connections: proven by a test protocol; 0.5 bar water pressure test report and 0.3 bar vacuum test report;

- Nominal diameter DN: OD (outside diameter) for diameter range DN/OD 160, DN/OD 200, DN/OD 250, DN/OD 315 and DN/OD 400;

- Readable and resistible marking, according the Standard EN1852-1;

- System: complete system – pipes, fittings;

- Compatibility with sewerage system elements ( manholes and inspection chambers, waste water treatment installations, drainage boxes);

- Compatibility with smooth pipes - DN/ OD  with guarantee water tightness of the connection;

- Active software that guarantees conformity with the standards of the product and the way of application for hydraulic(АТV А110)  and static (ATV127)calculations of the sewage pipe;

- Standard:  EN1852-1.

Technical specification: