INSPECTION CHAMBERS MADE OF INJECTION-MOLDED POLYPROPYLENE

- Product Description – constructed from separate injection-molded components with an external ribbed surface, connected together by welding or by an elastomer seal;

- Standard EN 13598-2:2020/NA:2022;

- Raw material used for the product – primary and certified by an independent authority;

- Material – polypropylene (PP);

- Nominal transverse stiffness of the riser ring SN ≥ 2kN/m2; certificate and test protocol from an independent institution in an EU member country;

- Mechanical strength of the cone tested according to EN ISO 13266:2023;

- Color: different from black, consistent in terms of shade and intensity;

- Mechanical strength of the connections for inlets and outlets according to EN ISO 13264:2017;

- Connection angles:

  - In the base – any angle from 90 to 270 degrees relative to the outlet;

  - In height – any angle from 0 to 360 degrees relative to the outlet.

- Possibility of including a higher level for the inlet relative to the outlet – cascade type chambers with a drop from 0.50 up to 6m;

- Maximum connection diameter: DN/ID 600;

- Possibility of different diameters for the inlets relative to the outlet – alligned vertex-to-vertex;

- Possibility for telescopic cover;

- Software for hydraulic modeling of the flow profile and 3D printing. Each profile, regardless of type, height, diameter, and connection angle, has optimal hydraulic performance;

- Burial depth according to the standard;

- Installation in groundwater up to 2m above the chamber bottom;

- Built-in stairs (steps) in the extension structural elements;

- Possibility to adjust the design height by reducing the extension structural elements;

- Guaranteed watertightness of the chamber and its connections to the sewer system;

- Connection method with the sewer network: coupling and sealing ring;

- Compatibility with profiled PP-B pipes and smooth-walled PVC and PP pipes;

- Test protocols from testing according to standard EN13598-2;

- Readable and durable marking of elements according to standard EN13598-2.