SADDLE WITH SCREW FOR LATERAL CONNECTION TO

DOUBLE-LAYERED CORRUGATED SEWER PIPE

- Application: for joining a branch sewer to an existing one or for installing a new one.

- The product is suitable for use as a connection fitting for branch sewers in buildings or for rain drainage piping as necessary.

- Description of product: a fitting made of the following components:

  - Body:

    - Inlet – it is a socketed inlet with a sealing ring, which serves to join the inlet sewer.

    - Middle section – it has threaded external surface intended for mounting the clamp

    - Outlet (end) - the end of the saddle is equipped with a sleeve which serves to ensure the water tightness of the bond between the inlet sewer and the collector where it will be joined.

  - A SADDLE type ring with a flat top and an bowed bottom having the diameter of the pipe where the saddle will be mounted

  - Clamp -  it is mounted in the middle of the body and serves to fix the saddle to the pipe

  - Sleeve – it is fixed to the flange and serves to ensure the water tightness of the bond.

- Manufacturing: The product is mould cast.

- Materials:

  - Body, clamp and sectional nut – PVC

  - Sealing ring at the socket and a rubber sleeve at the outlet (end) – EPDM 45  ±5

- Diameters and type of the inlet pipe – DN/OD160 and DN/OD200

  - Smooth-wall PVC and PP pipes

  - Corrugated pipes using an additional adaptor

- Diameter of the outlet pipe where the saddle is mounted –

  - DN/OD160, DN/OD200, DN/OD315, DN/OD400, DN/ID500, DN/ID600, DN/OD800, DN/OD1000

- Profile height of the point of joining – up to 100 mm

- Type of outlet pipe where the saddle is mounted – Pragma type corrugated pipes are manufactured in accordance with BDS EN 13476 – 1,2,3:2009

- Water tightness – from – 0.3bar to 0.5bar

- Standards:  DIN EN 1401-1:1998-12, DIN 19 543-3:2000-07, 13476-1, BDS EN1 1277, EN12256, EN 1053,

- Certificates and approvals:  MPA – K 075/05; CSTB  -29/1-MR-189; DIBT Z-42.1-382

- Production: in accordance with ISO 9001

- Technical specifications:

| DN | DN inlet sewer PP or PVC pipe | DN outlet sewer corrugated РР pipe |
| --- | --- | --- |
| DN/OD | 160 | DN/OD160 | up to DN/ID1000 |
| DN/OD | 200 | DN/OD200 | up to DN/ID1000 |